## Slide 1: NVT45 – 10_02 – Diode
Diode (triangle vs flat); Radius of curvature = 23nm; Gap = 12nm; Thickness = 5nm Cr + 25nm Au; angle of the triangle = 37deg

## Slide 2: NVT45 – 02_01 – Bowtie
Bowtie; Radius of curvature = 20nm; Gap = 27nm; Thickness = 5nm Cr + 25nm Au; angle of the triangle = 37deg